## Slide 1: Mueller Matrix Spectra to CD by Machine Learning
Results on synthetic data, and what is missing before real data
2026-10-10 · Every number is from synthetic spectra; no measured data has been used yet
M00
M01
M02
M03
M10
M11
M12
M13
M20
M21
M22
M23
M30
M31
M32
M33
TE
TM
Notes: Cover. The grid shows the 18 input channels: 16 Mueller elements measured at 65 degrees oblique incidence, plus TE and TM at normal incidence.

## Slide 2: At the theoretical limit, on synthetic data only
< 0.01%
Errors above 0.3 nm
0.65% with the CNN alone
0.067 nm
CD RMSE after refinement
Equal to the theoretical lower bound of 0.067 nm
0
Real samples verified
Every conclusion still needs real data
Helps: refinement (largest gain), MLP in place of CNN, cross-channel information
Little effect: deeper or wider networks, ensembles, more than 5,600 training spectra
Largest gap: real file format unconfirmed, and far more labels needed than TEM usually provides
Notes: Three figures: the best synthetic result, the share of samples beyond 0.3 nm, and the absence of any real-data verification. Acceptance: every sample within 0.3 nm first, RMSE second.

## Slide 3: Method: network estimate, then a model fit
Spectrum
18 channels × 101 wavelengths
Network
MLP or multi-channel 1D CNN
Initial CD
One forward pass
Refinement
Least-squares fit to the forward model
CD ± error
Plus a misfit warning
No RCWA needed
A second network is trained on the same data in reverse, CD to spectrum. The regression averages the noise out.
Yardstick: Cramér–Rao bound
The smallest error any unbiased estimator can reach at a given noise level. It shows how much room is left.
Data: synthetic spectra
CD 20–80 nm, noise 0.01. Not a physical simulation; used to validate the pipeline and compare methods.
Notes: Two stages: the network gives an initial CD, then Gauss-Newton fits it against a forward model learned from the same training data.

## Slide 4: MLP plus refinement reaches the bound
Chart: CD RMSE (nm), lower is better
| CNN baseline | CNN, 3-model ensemble | CNN, noise augmentation | MLP | MLP, 3-model ensemble | MLP + refinement | Theoretical bound
CD RMSE (nm) | 0.105 | 0.097 | 0.095 | 0.077 | 0.074 | 0.068 | 0.067
1
The CNN is noise-sensitive
1.57 times the bound. Normalization, pooling, width and learning rate all land between 0.102 and 0.132 nm.
2
The MLP gets to 1.15 times
Possibly because synthetic spectra lack local structure; this must be re-tested on real spectra.
3
Refinement gets to 1.02 times
The ranking is the same for three other synthetic physics settings.
Only CD varies; 5,600 training spectra; scored on 20,000 fresh spectra
Notes: Main comparison. Bound 0.067 nm; CNN 0.105, MLP 0.077, with refinement 0.068.

## Slide 5: Error rises sharply below about 700 training samples
Chart: CD RMSE (nm) by number of training samples
| 106 | 210 | 420 | 700 | 5,600
MLP | 0.305 | 0.24 | 0.178 | 0.132 | 0.077
MLP + refinement | 0.502 | 0.413 | 0.161 | 0.089 | 0.068
1
Refinement hurts below 700
The forward model is not accurate enough yet. Training compares both on validation data and picks automatically.
2
The CNN needs more data
0.290 nm at 700 samples, 0.105 nm at 5,600, and flat beyond that.
3
What it means for real data
With only tens of TEM values, expect errors above 0.3 nm; another source of labels would be needed.
Only CD varies; labels without error; theoretical bound 0.067 nm
Notes: Sample count is the key constraint for real data. The third point is inferred from the synthetic results and not yet confirmed on real data.

## Slide 6: Refinement adds error bars and absorbs offsets
Chart: CD RMSE (nm) by wavelength-axis offset
| 0 nm | 0.2 nm | 0.5 nm | 1.0 nm
MLP | 0.077 | 0.099 | 0.176 | 0.329
Refinement, offset fitted | 0.072 | 0.072 | 0.071 | 0.071
1
The offset is fitted too
A 1 nm wavelength offset quadruples the network's error; fitting the offset alongside CD removes the effect.
2
The error bar is calibrated
Actual error divided by predicted standard deviation has a spread of 1.03, against an ideal 1.00.
3
Unusual spectra are flagged
With doubled noise 100% of spectra are flagged, against 0.02% of normal ones.
Only CD varies; 5,600 training spectra
Notes: Beyond accuracy, refinement gives a per-spectrum error bar, a misfit warning, and robustness to wavelength calibration offsets.

## Slide 7: TEM label error of 0.3 nm is tolerable; 1 nm is not
No label error
0.077
0.068
MLP
With refinement
Close to the 0.067 nm bound
Label error 0.3 nm
0.117
0.076
MLP
With refinement
Refinement is barely affected
Label error 1.0 nm
0.258
0.178
MLP
With refinement
Both clearly worse
Label error passes to the network
The network learns the erroneous labels; the error is not averaged out.
Refinement averages it out
With 16,800 training spectra the 0.3 nm case reaches 0.072 nm.
Range edges biased at 1 nm
The interior stays at 0.077 nm, so train on a wider range than is used.
CD RMSE (nm). Only CD varies; 5,600 training spectra; test labels without error
Notes: TEM label error is simulated as Gaussian. The size and distribution of real TEM error still need to be established.

## Slide 8: Labels for other parameters are valuable
Chart: CD RMSE (nm) with 3 nuisance parameters
| CNN | MLP | MLP, multi-task | Refinement, CD labels only | Refinement, all labels | Theoretical bound
CD RMSE (nm) | 0.154 | 0.133 | 0.122 | 0.125 | 0.096 | 0.09
1
The bound itself rises
From 0.067 to 0.090 nm. Three extra parameters stand in for height, sidewall angle and film thickness.
2
With their labels: near the bound
Refinement reaches 0.096 nm; the multi-task network 0.122 nm.
3
CD labels only: position matters
0.098 nm in the central 70% of the training range, but 0.187 nm in the outer 3%, worse than the network's 0.161.
16,800–33,600 training spectra; the nuisance parameters are generic stand-ins, not physical models
Notes: The nuisance-parameter case is closest to real measurement. With CD labels only, the manifold method helps only when the training range is clearly wider than the range in use.

## Slide 9: Which ML methods help, on synthetic data
Method | Change in CD RMSE | Verdict
Refinement (learned forward model) | 1.57× bound → 1.02× | Helps most
MLP in place of CNN | 1.57× bound → 1.15× | Helps; re-test on real data
Cross-channel vs. per-channel convolution | 0.105 vs. 0.138 nm | Cross-channel helps
Noise augmentation, ensembles | 0.105 → 0.095 / 0.097 nm | Small gain
Multi-task: also predict other parameters | 0.133 → 0.122 nm | Small gain; needs labels
Depth, width, normalization, pooling, more data | No clear change | No effect
Channel attention, 2D / 3D CNN | 0.105 → 0.108 / 0.111 / 0.119 nm | No effect
First-derivative features | CNN 0.105 → 0.121, MLP 0.077 → 0.096 | Worse
Original question (is cross-channel information among the Mueller elements useful?): yes within a CNN, but an MLP reading every channel directly does better
Notes: The attention gates all settled near 1, so every synthetic channel is equally informative. The 2D and 3D CNNs use narrower layers because of CPU cost.

## Slide 10: Real data: code is ready, data is missing
Data still needed
1
One real spectrum export
Confirms format, wavelength range, channel count
2
Number of spectrum–TEM pairs
Below a few hundred, another label source is needed
3
Repeat measurements of one site
To estimate the real measurement noise
4
What comes with each TEM value
Wafer ID, plus height, sidewall angle and similar
5
A wide enough sampling range
Train on a wider range than will be used
Code ready, awaiting real data
1
Training on real data
A folder of spectra plus a reference-CD table
2
Cross-validation
Grouped by wafer; suited to small sample counts
3
Method comparison tool
Every method scored on the same splits
4
Install and handoff documents
Pinned versions, intranet install, notes for the next agent
5
Still to do
Re-run every comparison on real data
Notes: Acceptance is set: every sample within 0.3 nm first, RMSE second. The real-data pipeline has so far only been tested on files written from synthetic spectra.